## Slide 1: Developments in Electroactive Lens Technology for Vision Correction
Harry Milton, Anthony Van Heugten
eVision Smart Optics
Display Week
May 16th, 2019

## Slide 2: Introduction to Liquid Crystal Lenses
Liquid crystal lenses are designed to change their focal length electronically
  Can be turned on and off
  Able to be switched between focal lengths
Why is this useful?
    Imaging applications
    Augmented reality applications
    Vision correction
Electronic vision correction
    Especially useful to correct presbyopia
    Video taken using eVision liquid crystal lens
Slide 1: Introduction to Liquid Crystal Lenses

## Slide 3: Introduction to Presbyopia Corrections
Presbyopia is the age related deterioration of the eye
  Reduction of flexibility in the crystalline lens
  Natural part of the aging process and affects all people over the age of 55
Current state of correction
  Most common correction is the use of reading glasses
  Correction is particular problematic for contact lens wearers.
Liquid crystal lenses show great potential for correcting presbyopia
  Able to provide additional focal power when required
  Analogous to putting on and removing a pair of reading glasses
Slide 2: Introduction to Presbyopia Corrections

## Slide 4: Vision Correction using Liquid Crystal Lenses
Contact Lenses
  Required to be thin
    (<300 micron)
  Able to be placed on the eye
  Compatible with existing contact lenses
Slide 3: Vision Correction using Liquid Crystal Lenses
Spectacle Lenses
  Need to have large optical area
    (25 mm upwards)
  Off axis performance important
  Able to be mounted into spectacle frames
Unique challenges when working with spectacle lenses and contact lenses
Requirements for both devices:
  Need to provide up to +3.00 D when activated
  Optically inactive when turned off
  Low voltage and power consumption

## Slide 5: Liquid Crystal Contact Lenses
eVision liquid crystal contact lens utilizes diffractive optical design
  Surface relief structure fabricated on polymer substrates
  Liquid crystal index matched with substrate
  6 mm optical zone
Lens has dimensions and curvature appropriate for contact lens use
  Fabricated using ophthalmic materials
  Radius of curvature to match the eye
  Lens design has appropriate thickness for contact lens use
    Lens prototype approximately 150 microns in thickness
  Electro-optical layers provide electric potential to liquid crystal layer
Slide 4: Liquid Crystal Contact Lenses

## Slide 6: Optimizing Contact Lens Optics
When using single point diamond turning – size matters
  Small diamond point is required to produce high quality diffractive structure
    Used for molds and prototyping
  However, small diamond points impact surface quality
  Hybrid approach implemented to give the best of both worlds
VAN Photoalignment
  Buffing process is problematic
  Many issues solved by use of photoalignment in contact lens device
  Exposure to polarizer UV light induces pretilt angle and ensures unidirectional switching
  Significant increase in optical quality when switching to VAN photoalignment
Slide 5: Optimizing Contact Lens Optics

## Slide 7: VAN Photoalignment
Slide 6: VAN Photoalignment
Off State On State

## Slide 8: Contact Lens in Action
Slide 7: Contact Lens in Action

## Slide 9: Contact Lens in Action
Slide 8: Contact Lens in Action

## Slide 10: Contact Lens in Action
Slide 9: Contact Lens in Action

## Slide 11: Contact Lens: Summary
Slide 10: Contact Lens: Summary
Four optical power states, for example:
  0.00 D when unpowered for distance vision
  +1.00 D for intermediate vision
  +2.00 D for near-intermediate vision
  +3.00 D for near vision
  Other combinations or more if needed
Switching Speed: 50 ms
Electrical power consumption: <2 μW
Able to be controlled via Bluetooth and remote control
  Cell phone and smart watch control developed
  Electronics under development for self contained unit

## Slide 12: Liquid Crystal Spectacle Lenses
Two primary approaches:
Slide 11: Liquid Crystal Spectacle Lenses
Surface Relief
  Similar technique to contact lens device
  Can be indexed matched to other liquid crystal modes such as chiral nematic
Electrode Based
  Uses flat substrates
  Photolithography used to develop electronic components
  Concentric ring electrodes are powered to product a gradient index optical device

## Slide 13: Surface Relief Spectacle Lenses
Slide 12: Surface Relief Spectacle Lenses
Single liquid crystal layer used with a diffractive structure
  Short pitch chiral nematic used
  Average liquid crystal refractive index observed – polarization insensitive
  Electrical switching reduces refractive index and induces optical power
  1st generation product able to provide additional +0.75 D when activated
  Optical zone is approximately 2 cm by 1 cm
  Next generation device to have higher power and larger optical zone
Currently used in TouchFocus™ spectacle lenses

## Slide 14: Spectacle Lens in Action
Slide 13: Spectacle Lens in Action

## Slide 15: Spectacle Lens in Action
Slide 14: Spectacle Lens in Action

## Slide 16: Electrode Based Spectacle Lenses
Slide 15: Electrode Based Spectacle Lenses
Currently in development
  Two primary modes of operation +1.00 D and +2.50 D with tuneable focus
  Uses photolithography to form electrode structure
  Individual electrodes used to form a GRIN lens
  To increase optical power phase resets are used
  To minimize the amount of connections required ITO connections are used
30 mm lenses able to be fabricated

## Slide 17: Vision Correction in Space
Slide 16: Vision Correction in Space
Visual impairment from intracranial pressure
  First discovered when astronaut in the International Space Station saw Earth less clearly
    Vision improved with reading glasses
  Shift in vision towards farsightedness
    Unpredictable during course of mission
One of the biggest challenges for the NASA Mission to Mars project
  Spaceship engineering is only half the problem – humans aren’t built for space travel
  Two potential show-stoppers for prolonged travel
    Radiation exposure
    Vision impairment from intracranial pressure (VIIP)
    Current studies are only 6 months – Mars mission is 2-3 years
What is the cause of this vision deterioration?

## Slide 18: Vision Correction in Space
Slide 17: Vision Correction in Space

## Slide 19: Vision Correction in Space
Slide 18: Vision Correction in Space
Best case is to prevent this from happening
  Back-up plans are in effect to correct vision loss from VIIP
Back up plan is adjustable spectacles
  Liquid crystal technology is capable of correcting multiple hyperopic shifts
  Only a single optic is required, with the lens being able to be programmed inspace
  eVision Smart Optics is currently working on this

## Slide 20: Summary and Conclusions
Slide 19: Summary and Conclusions
Liquid Crystal Lenses demonstrated solution for Presbyopia correction
Contact Lens Form
  High quality optical devices formed using diffractive surface relief structure
  Photoalignment improves optical performance
  Up to +3.00 of optical power demonstrated
  Tunability also demonstrated for intermediate vision correction
Spectacle Lens Form
  Bifocal spectacle lenses already commercialized
  Larger scale tunable lenses under development
  30 mm lenses able to be fabricated using electrode based structures
  Up to +2.50 D of tunable focus shown in large scale lenses

## Slide 21: Thank you for Listening!
Slide 20: Finish
Contact Information:
  Info@evisionoptics.com
  Hmilton@evisionoptics.com
Website:
  www.evisionoptics.com
Location:
  1144 Tallevast Road, Sarasota, Florida, 34243, USA